# System  5000 DOUBLE SLIDER with THERMAL BREAK

Supply and fitting of sliding windows and doors comprising of 6063 aluminium alloy profiles with T5 thermal treatment.

The frame and sash have a sectional area of 199 mm & 28 mm respectively, both in windows as in doors.  The average aluminium profile wall thickness is 1.5 mm.

The aluminium profiles are designed to be thermally broken which is achieved by inserting polyamide 6.6 isolation strips, 24 mm wide that are reinforced with 25% fibre glass.

This system also incorporates a central shutter guide rail.

Classifications achieved at test centre*:

Air permeability according to EN 12207:2000		Class  3

Water tightness according to EN 12208:2000 		Class  8A

Wind resistance according to EN 12210:2000		Class  C4

* Test reference 1,25  x 1,50 m. 2 Sashes.

Surface Finish:

-Powder coating in ..……….   carried out with a complete cycle that includes de-greasing, strip clean in a bath of caustic soda, wash, controlled oxidisation, drying and thermocoated using polyester powder applied electrostatically and a subsequent curing at 200 ° C. The quality of the paint coating is guaranteed by the QUALICOAT seal of approval and the thickness is between 60 & 100 microns.

-Anodized, finish………..  colour............ carried out with a complete cycle that includes de-greasing, wash, anodic oxidation, coloring and sealing operations. The thickness and quality of the anodic coating is guaranteed by EWAA-EURAS seal with a minimum class……... microns.