# System  BALUSTRADING

Supply and fitting of balustrades comprised of aluminium alloy 6063 profiles with T5 thermal treatment.

A load bearing structure made by anchoring COR-8502 handrails and COR-8507 40 x 20 mm columns that are distanced ………… mm apart and fixed using 908515 type fixings.

Style:

- Total glass balustrade with COR-8509 with 80 mm external perimeter elliptical handrail.

- Glass balustrade with a free top edge and COR-8520 square shape handrail 60 mm wide/ COR-8510 circular shape (66 mm diameter) / COR-8501 elliptical handrail (80 mm external perimeter)

- Vertical post balustrade type COR-8508 and COR-8520 square type handrail (60 mm wide) / COR-8510 circular shape (66 mm diameter) / COR-8501 elliptical shape (80 mm external perimeter)

- Vertical post balustrade with free top edge and COR-8520 handrail (60 mm wide) / COR-8510 circular shape (66 mm diameter) / COR-8501 elliptical shape (80 mm external perimeter)

Classifications achieved at test centre*:

According to UNE 85.237-1991, UNE 85.238-1991, UNE 85.240-1990 norms and requisites established by the Technical Building Code (DB SU-1 and DB SE-AE).

- Static horizontal test towards the outside

- Static horizontal test toqards the inside

- Static vertical test

- Dynamic soft body test

- Dynamic hard body test

- Verification of section 3.2 of the DB SE-AE from the Technical Building Code

- Security test

Class A – EXCELLENT (UNE 85.240-1990)

*Test reference on total glass balustrade 1.1 (H) x 2.45 (L) mts and 3 posts.

*Test reference on a balustrade and post system with free top edge 1.1 (H) x 2.0 (L) mts. and 3 columns

Surface Finish:

-Powder coating in ..……….   carried out with a complete cycle that includes de-greasing, strip clean in a bath of caustic soda, wash, controlled oxidisation, drying and thermocoated using polyester powder applied electrostatically and a subsequent curing at 200 ° C. The quality of the paint coating is guaranteed by the QUALICOAT seal of approval and the thickness is between 60 & 100 microns.

-Anodized, finish………..  colour............ carried out with a complete cycle that includes de-greasing, wash, anodic oxidation, coloring and sealing operations. The thickness and quality of the anodic coating is guaranteed by EWAA-EURAS seal with a minimum class……... microns.