# System CORTIZO COMPOSITE PANEL

Supply and fitting of cladding based on trays made with sheets of Cortizo aluminium composite panel PE or FR with a total thickness of 4 mm formed by an external and internal double aluminium lamínate, 0.5 mm thick and in alloy 3005H44 / 3105H44 / 3105H46 o 5005H22 with a 3 mm intermediate polyethelene nucleus.  The aluminium is painted on the external surface with PVDF Kynar 500 25/35 micron paint  in ……………..colour with a plastic film protection. The interior aluminium is painted with a primer protection.  Also included is the punching, drilling and cutting of the sheets in order to shape the aluminium composite trays to the necessary dimensions.

Horizontal and vertical panel adjustment in a length of ………. mm and ………… in width. Clearance between each tray is between 8-10 mm.

Load bearing structure comprising of the construction elements such as the aluminium alloy 6063 T5 profiles in omega shape, hanging supports and double T fixing, stainless steel screws, rivets, anti-vibration gaskets that allow a fixing system according to the building project needs.

Surface finish:

Colour  painted………………….using paint for high resistance to corrosion and ageing.

- PVDF Kynar 500 (polyvynil flouride) (70/30) 2 coated for high flexibility and resistance to UV rays

- High-density polyethylene (HDPE)

or

-PVDF Kynar 500  (polyvynil flouride) (70/30) 3 coated especial for aggressive environments.

The quality of the  paint coating presents a thickness of between 25 & 35 microns.