# System COR-URBAN CC with THERMAL BREAK

Suplly and fitting of Cortizo Groove hinged windows comprising of 6063 aluminium alloy profiles with T5 thermal treatment along with exclusive Cortizo Groove opening kits and accessories guaranteeing that it functions well along with the results obtained from the tests.

The frame and sash have a section area of 122 mm & 121 mm respectively.  The maximum sash glazing is 18 mm meanwhile the internal sash can be glazed up to 28 mm.  The average aluminium wall thickness is 1.6 mm.

The aluminium profiles are provided with a thermal break by inserting 35 mm polyamide 6.6 isolation strips in the frame and 20 mm in the sash reinforced with 25% fibre glass.

Weather tightness is achieved using a quadruple system of EPDM gaskets.

Classifications achieved at test centre*:

Air permeability according to EN 12207:2000		Class  4

Water tightness according to EN 12208:2000 		Class  E1650

Wind resistance according to EN 12210:2000		Class  C5

* Test reference 1,23 x 1,48  m. 1 Sash.

Surface Finish:

-Powder coating in ..……….   carried out with a complete cycle that includes de-greasing, strip clean in a bath of caustic soda, wash, controlled oxidisation, drying and thermocoated using polyester powder applied electrostatically and a subsequent curing at 200 ° C. The quality of the paint coating is guaranteed by the QUALICOAT seal of approval and the thickness is between 60 & 100 microns.

-Anodized, finish………..  colour............ carried out with a complete cycle that includes de-greasing, wash, anodic oxidation, coloring and sealing operations. The thickness and quality of the anodic coating is guaranteed by EWAA-EURAS seal with a minimum class……... microns.