# System  EQUITY CURTAIN WALL

Supply and fitting of profiles for a light façade comprising of general modules dimensioned at  …………. formed by ……………. vision zones and made from 6063 aluminium profiles with T5 thermal treatment.

A load bearing structure comprsing of mullions dimensioned according to a static calculation type Cor-9351 or Cor-9354 and transoms type Cor-9341 or Cor-9344 according to the specific building needs.  Both have a seen surface area of 18 mm and include drainage and ventilation channels and are joined by end caps with expansión gaskets at both ends.

Glazing is based on the Cor-9140 profile that compresses the glass around its perimeter and fixing it to the load bearing structure. Finally, Cor-9133, Cor-9139, Cor-9142, Cor-9143, Cor-9183 & Cor-9198 embellishment covers are fitted horizontally or vertically that gives an end result of a 52 mm external seen surface.

Optimum weather tightness is achieved by using a triple barrier made from EPDM gaskets.

Thermal insulation by way of 24 mm insulation pieces.

Surface Finish:

-Powder coating in ..……….   carried out with a complete cycle that includes de-greasing, strip clean in a bath of caustic soda, wash, controlled oxidisation, drying and thermocoated using polyester powder applied electrostatically and a subsequent curing at 200 ° C. The quality of the paint coating is guaranteed by the QUALICOAT seal of approval and the thickness is between 60 & 100 microns.

-Anodized, finish………..  colour............ carried out with a complete cycle that includes de-greasing, wash, anodic oxidation, coloring and sealing operations. The thickness and quality of the anodic coating is guaranteed by EWAA-EURAS seal with a minimum class……... microns.