# System MALLORQUINA

Supply and fitting of mallorquina windows/doors shutters…………… and Euro Groove comprising of ………. sashes type………………. made with 6063 alloy aluminium profiles and T5 thermal treatment.

The frame and sash have a depth of 40 mm and 48 mm respectively both in windows as in doors.  The average wall thickness of the aluminium profiles is 1.3 mm in windows and 1.4 mm in doors.

Extruded security shutters, fixed or adjustable.

Classifications achieved at test centre*:

Wind resistance according to EN 13659:2004 norms		               Class 5

* Test reference 1.50 x 1.50 mts. double sash

Surface Finish:

-Powder coating in ..……….   carried out with a complete cycle that includes de-greasing, strip clean in a bath of caustic soda, wash, controlled oxidisation, drying and thermocoated using polyester powder applied electrostatically and a subsequent curing at 200 ° C. The quality of the paint coating is guaranteed by the QUALICOAT seal of approval and the thickness is between 60 & 100 microns.

-Anodized, finish………..  colour............ carried out with a complete cycle that includes de-greasing, wash, anodic oxidation, coloring and sealing operations. The thickness and quality of the anodic coating is guaranteed by EWAA-EURAS seal with a minimum class……... microns.