# System  MILLENNIUM FR DOOR with THERMAL BREAK

Supply and fitting of hinged doors that have a fire resistance classification of class EI260 comprising of 6063 aluminium alloy profiles with T5 thermal treatment.

The frame and sash both have an 80 mm section with an average aluminium profile thickness of 2.2 mm. The sash and frame are both coplanar.

The two or three barrel hinges will support weights of up to 240 kgs. per sash.

The aluminium profiles are ready for thermal breaking by inserting 35 mm wide polyamide 6.6 isolation strips re-inforced with 25% fibre glass both in frame as in sash. The profile chambers are filled with non-combustible retarding insulation materials. The gaskets are intumescent with a dilating effect and in the glazing area with biosoluble paper is built in.

Classifications achieved at test centre*:

Fire resistance and smoke control

EN 1364-1:2000 & UNE-EN 1634-1:2010 norms

Class EI260 – C5

Classification according to EN 13501-2:2009+A1:2010 norms

(C5= 200.000 test cycles)

*Reference test carried out on 1.35 x 2.35 mts, single sash with 23 to 25 mm E160 single glazing

Surface Finish:

-Powder coating in ..……….   carried out with a complete cycle that includes de-greasing, strip clean in a bath of caustic soda, wash, controlled oxidisation, drying and thermocoated using polyester powder applied electrostatically and a subsequent curing at 200 ° C. The quality of the paint coating is guaranteed by the QUALICOAT seal of approval and the thickness is between 60 & 100 microns.

-Anodized, finish………..  colour............ carried out with a complete cycle that includes de-greasing, wash, anodic oxidation, coloring and sealing operations. The thickness and quality of the anodic coating is guaranteed by EWAA-EURAS seal with a minimum class……... microns.