# System  MEDITERRÁNEA BALCONY

Supply and fitting  of sliding windows and doors comprising of 6063 aluminium alloy profiles with T5 thermal treatment

The frame and sash have a sectional area of 106 & 45 mm respectively both in windows as in doors.  The average aluminium profile wall thickness is 1.5 mm and up to 1.7 mm in critical load areas.

A system of perimetral windows and doors with mitre joins and comprising of a monorail sliding sash and a fixed sash with hidden rail.

Classifications achieved at test centre*:

Air permeability according to EN 12207:2000		Class  3

Water tightness according to EN 12208:2000 		Class  8A

Wind resistance according to EN 12210:2000		Class  C4

* Test reference 1,49 x 1,24  m. 1 Sahs + 1 Fix.

Surface Finish:

-Powder coating in ..……….   carried out with a complete cycle that includes de-greasing, strip clean in a bath of caustic soda, wash, controlled oxidisation, drying and thermocoated using polyester powder applied electrostatically and a subsequent curing at 200 ° C. The quality of the paint coating is guaranteed by the QUALICOAT seal of approval and the thickness is between 60 & 100 microns.

-Anodized, finish………..  colour............ carried out with a complete cycle that includes de-greasing, wash, anodic oxidation, coloring and sealing operations. The thickness and quality of the anodic coating is guaranteed by EWAA-EURAS seal with a minimum class……... microns.