# System MILLENNIUM CURTAIN WALL

Supply and fitting of profiles for a light façade comprising of general modules dimensioned at  …………. formed by ……………. vision zones and made from 6063 aluminium profiles with T5 thermal treatment.

A load bearing structure comprising of mullions type COR-9051 with a 65 mm seen surface that ensures perfect resistance to bending from wind action.

The external glazing is fixed using grampons and ball and socket joints.  The grampons are made from stainless steel and surround the ball and socket joints to which the glazing is fixed afterwards having been previously drilled so that it can be secured.  The grampons are fixed to the load bearing profile using a support and an aluminium counterplate.

Surface Finish:

-Powder coating in ..……….   carried out with a complete cycle that includes de-greasing, strip clean in a bath of caustic soda, wash, controlled oxidisation, drying and thermocoated using polyester powder applied electrostatically and a subsequent curing at 200 ° C. The quality of the paint coating is guaranteed by the QUALICOAT seal of approval and the thickness is between 60 & 100 microns.

-Anodized, finish………..  colour............ carried out with a complete cycle that includes de-greasing, wash, anodic oxidation, coloring and sealing operations. The thickness and quality of the anodic coating is guaranteed by EWAA-EURAS seal with a minimum class……... microns.