# Sistema  TAMIZ

Supply and fitting of window / door shutters with fixed or adjustable louvres comprising of ………….. sashes in hinged, folding, sliding modes made with 6063 aluminium alloy profiles and T5 thermal treatment

The frame and sash are 47 and 40 mm deep respectively both in windows as in doors.  The average wall thickness is 1.3 mm in windows and 1.5 mm in doors.

Fixed or adjustable extruded security louvres,

Classifications achieved at test centre*:

Wind loading resistance (UNE 13659:2004): CLASS 5

Reference test 1,5 x 1,5 m., 2 sashes.

Surface Finish:

-Powder coating in ..……….   carried out with a complete cycle that includes de-greasing, strip clean in a bath of caustic soda, wash, controlled oxidisation, drying and thermocoated using polyester powder applied electrostatically and a subsequent curing at 200 ° C. The quality of the paint coating is guaranteed by the QUALICOAT seal of approval and the thickness is between 60 & 100 microns.

-Anodized, finish………..  colour............ carried out with a complete cycle that includes de-greasing, wash, anodic oxidation, coloring and sealing operations. The thickness and quality of the anodic coating is guaranteed by EWAA-EURAS seal with a minimum class……... microns.