# System  VENTILATED STRUCTURAL CURTAIN WALL

Supply and fitting of profiles for a light curtain wall comprising of general modules of …………in dimension and made up of ……….. sight areas using profiles in 6063 alloy with T5 thermal treatment.

A load bearing structure comprising of mullions type COR-9553 with a seen surface of 50 mm that ensures perfect resistance to bending when subject to wind action and internal and external transoms type COR-9554 & COR-9555 respectively.

The external glazing is adhered to profile type Cor-2030 with special anodising, for gluing the structural sillicone and supported by frame support section ref. Cor-9525.

Optimum weather tightness is achieved by the use of a triple barrier made up of EPDM gaskets

The internal glazing in sash profile type COR-2085 for practical opening types.

The fixing is achieved by using three pieces of extruded aluminium that ensure a three dimensional adjustment which corrects any possible defects in the castings and resulting in a completely levelled façade.

Surface Finish:

-Powder coating in ..……….   carried out with a complete cycle that includes de-greasing, strip clean in a bath of caustic soda, wash, controlled oxidisation, drying and thermocoated using polyester powder applied electrostatically and a subsequent curing at 200 ° C. The quality of the paint coating is guaranteed by the QUALICOAT seal of approval and the thickness is between 60 & 100 microns.

-Anodized, finish………..  colour............ carried out with a complete cycle that includes de-greasing, wash, anodic oxidation, coloring and sealing operations. The thickness and quality of the anodic coating is guaranteed by EWAA-EURAS seal with a minimum class……... microns.